CERTIFICATE OF ANALYSIS

Date: 2021/11/23   S/C NO.2021MT166   Invoice No:2021MT166

Manufacturer：MIT-IVY INDUSTRY CO.,LTD

PRODUCT CODE: MT202110231122403
CAS ：112-24-3        MF:C6H18N4  HS code No.:29212900

Product Description: Triethylenetetramine

| order number | project | desired value | measured value | empirical method |
| --- | --- | --- | --- | --- |
|  |  | I mould | Ⅱ mould | I mould | Ⅱ mould |  |
| 1 | Foreign rules | Colorless to yellow, transparent and sticky liquid |  | qualified | Q/NDK 049-2018 |
| 2 | Triethyltetramine " Quality score)/% | ≥98.0 | ≥95 |  | 99.5 | Q/NDK 019-2018 |
| 3 | Water portion (mass fraction)/% | <1 | <3 |  | 0.8 | GB/T6283 |
| 4 | Chromscale (platinum-drill color) / h a zen unit | ≤50 | ≤50 |  | 20 | GB/T3143 |
| 5 | Density of 120.g/cm3 | 0.98-1.03 |  | 0.987 | GB/T4472 |
| 6 | Amine Value mgKOH/g | 1410 ~ 1480 |  | 1445 |  |
| 7 | Specific gravity (20/20°C) | 0.979 ~ 0.984 |  | 0.980 |  |
| : 1 Type 1 products are used for high use, and type products meet most uses. |
| Inspector: | conclusion Inspection department Inspection opening period: 11/23/2021 |

Total Quantity:1000g     Packaging:200kg/drum

Other Informations:N/A     OTHER REF(S): N/A   
The information we provide about our products does not imply any warranty or guarantee.Our general terms of business apply .This report was generated automatically and is valid without a signature.